## Slide 1: Science cases for neutron reflectometry
Tommy Nylander
Physical Chemistry
Lund University
Lund, SWEDEN
Email: Tommy.Nylander@fkem1.lu.se

## Slide 2: Acknowledgements to:
Kåre Larsson
Justa Barauskas
Giovanna Fragneto
Eric (Jianming) Zhang
Adrian Rennie
Arwel Hughes
Per Linse
Stefan Zauscher
Fredrik Tiberg
Bob Thomas
Marité Cardenas
Hannah Wacklin
Marie-Louise Ainalem
Bengt Jönsson
Pauline Vandoolaeghe
Richard Campbell
Emma Sparr
Agnes Michanek

## Slide 3: Application solid –liquid interface

## Slide 4: Approach to evaluate neutron reflectometry date (Example polymer brushes)
J. Zhang, T. Nylander, R. A. Campbell, A. R. Rennie, S. Zauscher, and Per Linse; Novel evaluation method of neutron reflectivity data applied to stimulus-responsive polymer brushes. Soft Matter 2008, 4, 500-509.

## Slide 5: Neutron reflectometry
Neutron Reflectometry gives density profile of the interfacial layer and selective deuteration + contrast matching gives composition
Neutron scattering strongly depends on isotope, e.g. hydrogen and deuterium => very different scattering
Reflectivity
q
Volume fraction
Distance from surface
What we measure!
What we want!
We need a model!!
q = (4p/l) sin q

## Slide 6: Polymer brushes (adapted from Per Linse)
D
l
D: distance between neighboring chain
l: brush height
D << 2RG for a brush (high density of brush) =>
Surface adsorption and solvency do
only slightly affect brush properties
Brush height, l, depends on two competing factors:
  1) Cost of stretching entropy => decrease the height
  2) Excluded volume interactions, “crowding” => increase height
Two simple analytic theories for non-adsorbing surface (grafted chains) and good solvent (high solubility of polymer):
  1) block segment density profile (Alexander 1977)
  2) parabolic segment density profile
  (Milner, Witten, and Cates (MWC)1988;
  Zhulina, Priamitsyn, and Borisov (ZPB) 1988)

## Slide 7: Neutron reflectivity: conventional evaluation
Reflectivity model*
R(q)
Fit to experiments
Improved fitting parameters
Initial fitting parameters:
polymer density thickness
roughness
Polymer volume fraction profile
*Including roughness
Layer model

## Slide 8: Modeling of the polymer brushes
establish model parameters to describing the interactions in an aqueous polymer solution from fitting to experimentally determined phase behavior
predict polymer brush density profiles using molecular-based lattice mean-field theory, developed by Scheutjens and Fleer, and Gunnar Karlström

## Slide 9: Neutron reflectivity: novel evaluation
Polymer brush theory
Reflectivity model
R(q)
Fit to experiments
Improved fitting parameters
Polymer volume fraction profile
Few parameters characterizing
the polymer system
Initial fitting parameters
length scale
grafting density

## Slide 10: Comparison of the two approaches
Advantages of the novel approach
  Fewer fitting parameters
  Good correlation between model and experiment:
    the experiments support the polymer theory
    the theory can be used to predict properties of the brush
    design of NR experiment for optimal outcome
Disadvantages of the novel approach
  Need of a suitable polymer brush theory
  Need of parameters characterizing the polymer brush
  Adapted software for the analysis of the NR data

## Slide 11: Fit of parameters characterizing the polymer
Fit of parameters describing interaction and internal degrees of freedom

## Slide 12: Predicted polymer volume fraction profiles
A large structural change at increasing temperature is predicted

## Slide 13: Characterization of surface without polymer
Si / SiO2 / solvent
Si / SiO2 / init layer / solvent

## Slide 14: Polymer brush: ILL data and models

## Slide 15: Parameters
Layer
model
Lattice
model
5 fitted parameters
2 fitted parameters
Common
to both models
1 fitted parameter

## Slide 16: Predicted reflectivity profiles in cmSi (note more features in this contrast as Silicon substrate is matched out and we only see the oxide and polymer layers)

## Slide 17: Calculated scattering length density profiles

## Slide 18: Some comments
Layer profile
  Fitting parameters
    Scattering length density
    Thickness
    Roughness
  Nonzero roughness in the reflectivity model is important
Lattice mean-field theory
  Fitting parameters (global)
    Length scale
    Grafting density (here experimentally unknown)
  Extensions
    Polyelectrolytes (e.g., polyacrylamide)
    Block copolymers
    Adsorbed polymers

## Slide 19: Summary
A novel evaluation method of NR data of polymer brushes based on model calculations of polymer brushes
A physical model is here invoked to handle the temperature-dependent polymer-solvent interaction of the thermo-responsive polymer
Same polymer model is used to evaluate the experimental data under different experimental conditions
Fewer fitting parameters as compared to the conventional layer model
The novel method can be utilized to optimize NR experiments

## Slide 20: Adsorption of liquid crystalline nanoparticles

## Slide 21: Lipid based self-assembled structures
Has a large potential as drug delivery systems:
Large capability to solubilise drugs
Can be dispersed into nano-sized liquid crystalline particles
Large variability of structures and morphologies - not only vesicles

## Slide 22: Self-assembled lipid liquid crystalline nanoparticle Beyond vesicles and liposomes
BARAUSKAS J, JOHNSSON M and TIBERG F (2005), `Self-assembled lipid
superstructures:beyond vesicles and liposomes', Nano Lett, 5, 1615-1619.

## Slide 23: Interfacial behavior of drug delivery vehicles are important for
the uptake of the drugs
the biocompatibility of the delivery system
stability upon storage.

## Slide 24: What happens when such a liquid crystalline nano particle meets a biological (model) membrane?
Glycerol monoolein (GMO) based dispersions (Cubosome®)
Dioleoylphosphatidylcholine (DOPC) supported bilayer
Bicontinuous cubic phase:
Curved lipid bilayer
+

## Slide 25: Main techniques used
Ellipsometry gives “optical” thickness and “dry” mass versus time
QCM-D gives “wet” mass with coupled water and dissipation measures the viscoelastic properties of the film
Neutron Reflectometry gives density profile of the interfacial layer and selective deuteration + contrast matching gives composition

## Slide 26: Adsorption on silica surface (simplest model of a hydrophilic surface

## Slide 27: Adsorption of CPNP on hydrophilic surfaces Nature of the interaction
Driving force is likely non electrostatic
However likely to be controlled by electrostatic repulsion interaction
Anchoring of intact nanoparticles
or
surface-induced nucleation and growth process
Vandoolaeghe, P., Tiberg, F., and Nylander, T., Interfacial behavior of cubic liquid crystalline nanoparticles at hydrophilic and hycrophobic surfaces. Langmuir, 2006. 22: p. 9169-9174.
 mg m-2
d Å
water
pH 2
0.1 M NaCl+ 0.01 M CaCl2

## Slide 28: Lateral organization of CPNP on silica surface imaged by fluorescence microscopy
Layer formed of patches
No lateral organization
Size roughly the same than nanoparticles
Vandoolaeghe, P., Campbell, R.A., Rennie, A.R., and Nylander, T., Adsorption of intact cubic liquid crystalline nanoparticles on hydrophilic surfaces − lateral organization, interfacial stability, layer structure and interaction mechanism. J. Phys. Chem C. 2009, 113, 4483-4494.
17.3 x 10.1 mm2

## Slide 29: Layer of CPNP on silica formed by intact particles
QCM-D
Viscoelastic properties
Large amount of acoustically coupled water
No phase transformation
vesicles
Large CPNP
Small CPNP

## Slide 30: CPNP layer structure on silica from neutron reflectivity
Single layer adjacent to the surface + repeating structure
SLD following a sinusoidal function versus z

## Slide 31: MODEL MEMBRANES: dDOPC or DOPC bilayers formed by vesicle fusion on a (negatively charged) silicon surface ≈ 90% coverage

## Slide 32: ADSORPTION OF CPNP ON DOPC BILAYER-ellipsometry
Initially observed a strong adsorption of the particles on the DOPC bilayer.
Subsequent decrease in the adsorbed amount
Adsorption/desorption of particles?

d
P. Vandoolaeghe, R. A. Campbell, A. R. Rennie, R. K. Thomas, F. Tiberg, F. Höök,
G. Fragneto, T. Nylander Adsorption of cubic liquid crystalline nanoparticles on model
membranes. Soft Matter, 2008 4, 2267–2277.

## Slide 33: ADSORPTION OF CPNP ON DOPC BILAYER-QCM-D
Maxima after one hour in the wet mass and change in dissipation (as for adsorbed amount from ellipsometry)
Change in dissipation is large and significantly more than from molecular adsorption
Adsorption/desorption of particles!
WHY?

## Slide 34: ADSORPTION OF CPNP ON d-DOPC BILAYER-neutron reflectivity (low CPNP conc)
Initial Bilayer
1.8
6
1.8
9
30
9
r
(10
-6
Å
2
)
d (Å)
Addition 0.05 mg/mL CPNP at pH 4: Integrity of bilayer seems to be kept but composition changes 20% solvent, 72% GMO, 8% DOPC
=>Lipid exchange occur
Reflectivity in D2O of d-DOPC (deuterated chains) bilayer after adding CPNP

## Slide 35: ADSORPTION OF CPNP ON d-DOPC BILAYER
Lipid exchange occur when CPNP attach to bilayer
This make interaction between CPNP less favorable
=> Detachment of some particles
Phase-diagram of D2O-DOPC-GMO
(from Gutman et al)

## Slide 36: DNA (Deoxy ribo nucleic acid)
  Store genetic information
  Highly Negatively charged polyelectrolyte
  Long L= 1.478 μm (Luciferase T7 Control
  DNA (4331bp))and stiff (RG= 155 nm. lp= 50 nm)

## Slide 37: Gene therapy requires that the large hydrophilic highly (negatively) charged DNA crosses the lipid membrane
Is this possible?
Compacting DNA with oppositely charge dendrimers (and surfactants)
  Reducing size
  Reducing charge
We have studied
  Compaction with surfactant in bulk at interfaces
  Transport of dendrimer across supported lipid bilayer
  Interaction of DNA/dendrimer complex with the bilayer
Can also be cationic
Surfactant micelles

## Slide 38: What happens when dendrimers interact with a model cell membrane?
or
or
Ainalem, M.-L.; Campbell, R.; Khalid, S.; Gillams, R.; Rennie, A.; Nylander, T. On the Ability of PAMAM Dendrimers and Dendrimer/DNA Aggregates to Penetrate POPC Model Biomembranes. J. Phys. Chem. B. 2010, 114, 7229-7244.

## Slide 39: Ellipsometry give change in adsorbed amount but not location
Increase in thickness and adsorbed amount when adding dendrimers (PAMAM-G4) to lipid (POPC) bilayer

## Slide 40: What happens when dendrimers interact with a model cell membrane?
or
Neutron reflectometry in D2O
Only possible fit with dendrimer under bilayer
44 Å, 85% D2O
28 Å, 8.4% D2O
5.5 Å, 19% D2O

## Slide 41: How does different generations of dendrimers interact with the bilayer?
Generation | M (g mol-1) | No charged groups | RH (Å)
2 | 3256 | 16 | 13.6
4 | 14215 | 64 | 24.5
6 | 58048 | 256 | 38.0

## Slide 42: The interaction with the bilayer depends on dendrimer generation
b,c
G2 (and G4) dendrimers penetrates bilayer but leaves it intact.
d
G6 partly penetrate bilayer but partly destroys it! The interaction with bilayer is stronger as the dendrimers partly adsorbs on top of the remaining bilayer.

## Slide 43: How do the dendrimers pass the bilayer?
Through defects?
Can they pass through the membrane? (AFM studies suggest this)
Corse grain simulation (Syma Khaled, University of Southampton)
Simulation (120 ns) using
GROMACS 3.3.1 simulation package
Parameters

## Slide 44: Coarse grain simulations: Dendrimers can pass through the membrane without “defects”?!
…and without the attractive force between dendrimer and the negatively charge silica surface
(confirmed by prel. experiments with free standing bilayers)
Additional simulations shows that the surface seems to slow down the process…
0 ns
30 ns
120 ns

## Slide 45: What happens when DNA/dendrimer complex interact with a model cell membrane?
No penetration of the bilayer by G4/DNA complex
G4/DNA complex sits on top of bilayer
or
430 Å, 77% D2O
28 Å, 8.4% D2O
5.5 Å, 19% D2O
Spanning bilayer
Beneath bilayer
Neutron reflectometry in D2O

## Slide 46: Conclusions
  Dendrimer interaction with model membranes
  G2 and G4 penetrates bilayers, but G6 partly destroys bilayer. Data supporting transfecting ability.
  Dendrimer/DNA complex interaction with model membranes
  Complex of G4 and G6 do not penetrate bilayers and G6 do not.
  Increasing ionic strength can release (G2) dendrimers form complex which penetrate bilayer
  Does the efficiency of dendrimers as transfection agent rest on their ability to penetrate the membrane?

## Slide 47: Neutron reflectometry at Liquid interfaces

## Slide 48: WHY STUDY SHORT RNA OLIGOMERS(miRNA)?
Important for regulatory properties in the cell, such as cell death, cell proliferation and for the initiation of several types of cancer.
There are significant amount of phospholipids in the cell nucleus and e.g. RNA in the nucleus is co-localize with these lipids.
Important for drug delivery, therapeutics, synthetic biology and fundamental understanding of biological mechanisms.

## Slide 49: OBJECTIVE: REVEAL MECHANISM AND CONSEQUENCES OF INTERACTION BETWEEN NUCLEIC ACIDS AND BIOMEMBRANES
We have studied the interaction of single stranded RNA (10 bases) and double stranded DNA (2000 base pairs)
  with monolayers (P= 8 and 28 mN/m) of
    zwitterionic DPPC (1,2-dipalmitoyl-sn-glycero-3- phosphatidylcholine)
    cationic DODAB (dioctadecyl-dimethyl-ammoniumbromide)
using surface film balance, fluroscence microscopy and neutron reflectometry.
Michanek, A.; Yanez, M.; Hughes, A.; Wacklin, H.; Nylander, T.; Sparr, E. “RNA and DNA association to zwitterionic and charged monolayers at the air-liquid interface” Langmuir, 2012, 28, 9621-9633

## Slide 50: Langmuir trough to record P-A isotherms
Wilhelmy plate to
record surface
pressure, P
Barriers to record
area per molecule, A

## Slide 51:  vs. Area isotherm of cationic DODAB monolayers on 2mM imidazole pH 7 with and without 0.06 mg/ml nucleic acids in sub-phase.
The presences of nucleic acids (NA) in the sub-phase only have minor effect on the isotherm shape
Isotherm shifted towards higher area indicating incorporation of nucleic acids.
P-A isotherm probe the interaction, but no information of the location of NA

## Slide 52: Neutron reflectometry can provide information on the location of nuclei acids on a lipid monolayer

## Slide 53: Reflectivity profiles for DODAB monolayer on 2mM imidazole, pH 7, with and without 0.06 mg/ml ssRNA or ds DNA
ssRNA (10b)
dsDNA (2000bp)
Low surface pressure, P=8.8 mN/m

## Slide 54: Reflectivity profiles for DODAB monolayer on 2mM imidazole, pH 7, with and without 0.06 mg/ml ssRNA or ds DNA
ssRNA (10b)
dsDNA (2000bp)
Hiugh surface pressure, P=28 mN/m

## Slide 55: Properties of monolayers and nucleic acids
Layer | d (Å) | R (Å) | SLD (10-6 Å-2) | Solv. % | A (Å2)
DODAB P=8.8 mN/m | 20 | 4 | -0.34 (6.23) | 42 | 96
DODAB P=28 mN/m | 20 | 4 | -0.34 (6.23) | 22 | 71
DPPC P=8.4 mN/m | 22 | 4 | 0.22 (5.53) | 32 | 83
DPPC P=28 mN/m | 22 | 4 | 0.22 (5.53) | 5 | 60
RNA (10b) |  |  | 3.6 4.5 D2O |  | 
DNA (2000bp) |  |  | 3.7 4.1 D2O |  | 
d = thickness, R = Roughness
SLD = Scattering length density (deuterated in paranthesis)
A=area per molecule from neutron data

## Slide 56: Fitting parameters

## Slide 57: Neutron reflectometry results show:
ssRNA (10 bases) penetrate and adsorb on top of the cationic DODAB at low P, but do no penetration at high P. Similar, but less extensive interaction with zwitterionic DPPC.
dsDNA (2000 base pairs) partially removes the cationic DODAB monolayer both at low P and high P. dsDNA forms thicker but less dense layer on the cationic DODAB than ssRNA.